## Slide 1
Survey Results
ESM Trainings
Webinars
Longer Remote Trainings
Online training Center
Winter Tech Assists
Stream Crossings: the good, the bad, and the
in-between
Dirt Gravel and Low Volume Road Program
WEBINAR
If you are reading this, then you are successfully seeing the webinar video. Webinar audio should be automatic through your computer (or click “join audio”), and options can be accessed in the “audio options” button on the bottom left. If your computer audio is not working, you can listen on your phone by dialing 646-876-9923.
2/11/21 Starts at 9am

## Slide 2
Road Aggregates 101
Note you can ask a question anonymously
Q&A
For audio via phone: 646-876-9923
2

## Slide 3
Road Aggregates 101

## Slide 4
Road Aggregates 101
  Purpose
  Introduce the updated “Aggregates 101” technical bulletin.
  Provide an introduction to commonly used road aggregates, especially for new CD staff.

## Slide 5
  Update and expanded “Aggregates 101” technical bulletin
Road Aggregates 101

## Slide 6
Road Aggregates 101
  Background
  Important Aggregate Properties
  Commonly Used Aggregates
    Coarse Aggregates
    Larger “rip-rap” aggregates

## Slide 7
Background
  Aggregate: A mixture of coarse to fine-grained particulate material used in construction, typically including sand, gravel, and crushed stone.
  Sources:
    Limestone
    Sandstone
Road Aggregates 101

## Slide 8
Background
  Making Aggregates:
    Blast
    Crush
    Sieve
Road Aggregates 101
https://www.geoengineer.org/news/last-blast-at-thornton-quarry-creates-a-new-reservoir

## Slide 9
Background
  Making Aggregates:
    Blast
    Crush
    Sieve
Road Aggregates 101
https://www.terex.com/finlay/en/product/jaw-crushers/j-1480

## Slide 10
Background
  Making Aggregates:
    Blast
    Crush
    Sieve
Road Aggregates 101
https://www.terex.com/finlay/en/product/jaw-crushers/j-1480
https://www.quarrymagazine.com/2020/03/19/blending-of-recycled-glass-and-crushed-rock-in-road-pavements/
Large size
Small size

## Slide 11
Background
  Gradation: Size distribution of particle in an aggregate by percent weight
  Example: AASHTO #1
    Mixture of 2-3 inch stones with no fine material
Road Aggregates 101
http://www.pennsysupply.com/construction-materials/aggregate.asp

## Slide 12
Background
  Gradation: Size distribution of particle in an aggregate by percent weight
  Example: AASHTO #1
    Mixture of 2–3 inch stones with no fine material
Road Aggregates 101
Everything must pass a 4” opening
Max 5% by weight can pass ¾” opening
At least 85% of material larger than 1.5”
https://laurelaggregates.com/products/aashto-1/

## Slide 13
Background
  Gradation: Size distribution of particle in an aggregate by percent weight
    Some Gradations can be crushed directly
    Some may have to be mixed after crushing
    Gradation is about size, It is independent of aggregate quality. Both good and bad parent material can be crushed to the same gradation.
Road Aggregates 101
Mixing 2A and fines to make DSA

## Slide 14
Background
  Gradation: Size distribution of particle in an aggregate by percent weight
  Open -vs- Well graded aggregates: drainage and compaction are mutually exclusive
Road Aggregates 101
http://www.martinstone.com/products/stone-modified/
Open-Graded (Clean)
Compaction? NO
Free draining? YES
Well-Graded
Compaction? YES
Free draining? NO

## Slide 15
Road Aggregates 101
  Background
  Important Aggregate Properties
  Commonly Used Aggregates
    Coarse Aggregates
    Larger “rip-rap” aggregates

## Slide 16
Aggregate Quality Properties
  Abrasion Resistance: Resistance to mechanical breakdown. Measured by “LA Abrasion”
Road Aggregates 101
Aggregate is placed in steel drum with steel spheres and rotated.
Results are expressed as % loss Lower % = less crushing = harder aggregate

## Slide 17
Aggregate Quality Properties
  Abrasion Resistance: Resistance to mechanical breakdown.
Road Aggregates 101
Abrasion resistance is most important for surface aggregates to resist traffic, grading, etc.
  Driving Surface Aggregate (DSA) (max LA Abrasion of 40)
  Anything used as a surface (most DOT aggregates range from 40-55)
Abrasion resistance less important if aggregate is to be buried or used off of the cartway.

## Slide 18
Aggregate Quality Properties
  Soundness: Resistance to weathering, specifically by freeze thaw cycles
Road Aggregates 101
Have you ever seen a rock do this is as little as one year?
That is poor soundness.

## Slide 19
Aggregate Quality Properties
  Soundness: Measured by Sodium Sulfate test
Road Aggregates 101
BEFORE
AFTER
Aggregate is soaked in sodium sulfate then dried 5 times, which mimic freeze thaw cycles.
Results are expressed as % loss Lower % = less breakdown = more sound aggregate

## Slide 20
Aggregate Quality Properties
  Soundness: Measured by Sodium Sulfate test
Road Aggregates 101
Soundness is most important for anything exposed to freezing temperatures
  Surface aggregates
  Shallow bases
  Rip Rap
  Shallow or exposed subsurface drains
  Anything not buried at least 18-32 inches
Soundness is less important for material buried below frost depth such as large fill projects.

## Slide 21
Aggregate Quality Properties
  Plasticity Index: PI is an approximation of clay in an aggregate
  Impacts of clay in aggregate
    Retain water
    Remains mobile (dust and sediment)
    Remain flexible (rutting)
Road Aggregates 101

## Slide 22
Aggregate Quality Properties
  Plasticity Index: PI is an approximation of clay in an aggregate
  Where does clay come from?
Road Aggregates 101
Are there clay seems in this limestone?
How much overburden may get mixed in?

## Slide 23
Aggregate Quality Properties
  Plasticity Index: PI is an approximation of clay in an aggregate
Road Aggregates 101
Plasticity is only run on material passing the #40 (<1mm)
Open graded or clean aggregate are “non plastic” by default
  Plasticity index
    0 = “non-plastic” (negligible clay / silt content)
    1-4 = some clay / silt
    4-6 = clay content can make material “sticky”
    6+ = starts to behave more like soil than aggregate

## Slide 24
IMPORTANT
  Abrasion Resistance, Soundness, and Plasticity are related to properties of the parent material.
    They can vary slightly from one rock face to another within the same quarry.
    They essentially remain the same regardless of the gradation or level of crushing done to the aggregate
Road Aggregates 101

## Slide 25
Road Aggregates 101
  Background
  Important Aggregate Properties
  Commonly Used Aggregates
    Coarse Aggregates
    Larger “rip-rap” aggregates

## Slide 26
Aggregates
  A word about specifications
Road Aggregates 101
AASHTO (American Association of State and Highway Transportation Officials) Federal spec on open-graded or clean stone
PA Specifications are maintained by PennDOT largely for well-graded aggregates (“Publication 408”, section 703).
note some redundancy, for example ASSHTO #1 = PA #4
Specifications that begin with an “R” designation are set by the National Crushed Stone Association.

## Slide 27
Common Coarse Aggregates
  PENNDOT 2A: well-graded
Road Aggregates 101
Designed as base for asphalt
Very common “standard” aggregate
2” top size
Fine content ranges from 0-10%
  Near 0, behaves almost as an open-graded aggregate
  Near 10, very well graded, approaching DSA
No plasticity specification
http://www.pennsysupply.com/construction-materials/aggregate.asp

## Slide 28
Common Coarse Aggregates
  PENNDOT 2A: well-graded
Road Aggregates 101
Uses
  Road base and subbase
  Pipe bedding
  Road fill (in areas where cost is low)
  Traditional road surface (not recommended due to variability of fines)
2A for crosspipe bedding
2A for road fill / base

## Slide 29
Common Coarse Aggregates
  PENNDOT 2A “Modified”
Road Aggregates 101
“Modified” does NOT exist as a spec.
Some quarries and townships will still use the term.
What is it?
  2A with extra fines
Purchase at your own risk since there is no spec.

## Slide 30
Common Coarse Aggregates
  PENNDOT 2RC: well-graded
Road Aggregates 101
Wide ranging in size and quality
Very common “standard” aggregate
2” top size
Fine content ranges from 0-30%
  Near 0, behaves almost as an open-graded aggregate
  Near 30…you just bought dirt
Can contain soil and even organics
Typically, high PI (lots of clay)
http://www.pennsysupply.com/construction-materials/aggregate.asp

## Slide 31
Common Coarse Aggregates
  PENNDOT 2RC: well-graded
Road Aggregates 101
Uses
  Pipe bedding / backfill
  Road fill
  Traditional road surface (not recommended due to variability of fines and clay content)
2RC for road fill / base
2RC for pipe bedding

## Slide 32
Common Coarse Aggregates
  Driving Surface Aggregate (DSA)
Road Aggregates 101
Like PennDOT 2A, BUT:
  Fine content is 10-17
  Stricter specs on abrasion resistance, soundness, and plasticity
  Additional specifications on placement
Designed for compaction and longevity as a wearing surface
2/4: Remote Training: “DSA Day”: Feb 4, 9am-noon

## Slide 33
Common Coarse Aggregates
  AASHTO #1 (PA#4)
Road Aggregates 101
Most used free-draining spec
Gradation
  Top size of 4”
  Only 15% can be smaller than 1.5”
  Only 5% can be smaller than ¾”
Uses
  Subsurface drainage
  Base stabilization
AASHTO # 1 for French Mattress
AASHTO # 1 for underdrain

## Slide 34
Common Coarse Aggregates
  Other Common Materials
Road Aggregates 101
Shale
Pit Run
Bankrun Gravel
These do NOT have a specification.
Typically excavated directly from ground with no processing.
They are highly variable in composition and quality
Primarily used as cheap sources of fill
http://www.millcreeksandgravel.com/crush-gravel http://mccollumtrucking.com/gravel/
Pit Run
Road Fill RFQ available on Center’s website
Bankrun Gravel
Shale as road fill

## Slide 35
Road Aggregates 101
  Background
  Important Aggregate Properties
  Commonly Used Aggregates
    Coarse Aggregates
    Larger “rip-rap” aggregates

## Slide 36
Common Coarse Aggregates
  Rip Rap
Road Aggregates 101
Generic Term for large clean stone
Used for stabilization (ditches, outlets, channels, banks, etc.)
R-3: (2" - 6")
R-4 (3" - 12")
R-5 (4" - 18")
R-6 (9" - 24")
R-7 (12" - 30")
R-8 (15" - 42")
http://www.pennsysupply.com/construction-materials/aggregate.asp
https://mmlime.com/materials/
https://mmlime.com/materials/
R-4
R-3
R-8

## Slide 37
Common Coarse Aggregates
  Rip Rap
Road Aggregates 101
http://www.pennsysupply.com/construction-materials/aggregate.asp
R-4
R-4 on bank slide stabilization
R-5 on ditch stabilization
R-7 on streambank stabilization

## Slide 38
Common Coarse Aggregates
  Other terms for Large Aggregate
Road Aggregates 101
These do NOT have a specification
Very roughly graded and highly variable
Terms you might hear:
  Surge: ~10” and smaller
  Shot Rock: essential rip-rap without a specification
  Gabion: similar to AASSHTO #1 /#3
http://mccollumtrucking.com/gravel/
“Surge”
“Shot Rock” as road fill

## Slide 39
Road Aggregates 101
  Additional Information
  DEP Watershed Academy
  “Rip-Rap” and Coarse Aggregate

## Slide 40
Road Aggregates 101
Crater Lake, Oregon

## Slide 41
Road Aggregates 101
Crater Lake, Oregon
2A pile in a flooded quarry pit!

## Slide 42
Survey Results
ESM Trainings
Webinars
Longer Remote Trainings
Online training Center
Winter Tech Assists
Road Aggregates 101
Dirt Gravel and Low Volume Road Program
WEBINAR
QUESTIONS ?
1/26-27: Remote ESM Training Jan 26 and 27, 8am-12:30 pm BOTH days:
1/28-29: Remote Administrative Training: 1/28 and 1/29, 9-11:30am BOTH days: Admin
2/4: Remote Training: “DSA Day”: Feb 4, 9am-noon: NEW
2/11: Webinar: Stream Crossings, the good, the bad, and the ugly: Feb 11, 9am: NEW
2/16-17: Remote ESM Training Feb 16 and 17, 8am-12:30 pm BOTH days:
2/18: Webinar: Annual Summary Report Overview: February 18, 9am: NEW
2/23: Remote Training: “Bookkeeper Bootcamp”: Feb 23, 9am-noon: NEW
2/25: Remote Training: “Streambank Stabilization”: Feb 25, 9am-noon: NEW