## Slide 1
DGLVR Workgroup
Proposed Driving Surface Aggregate Specification Changes
For technical assistance, call: 814-865-5355
If you are reading this, then you are successfully seeing the webinar video. Webinar audio should be automatic through your computer, and options can be accessed in the “audio options” button on the bottom left. If you are having audio issues, or are in a location where listening via phone is preferable, audio is also available on the CDGRS conference line at: 312-626-6799
2/2/23

## Slide 2
Background
DSA is only approved unbound surface aggregate for use with DGLVR funds
Specification is designed for maximum compaction density.
  Resist erosion
  Lengthen maintenance cycles
  Less sediment runoff
Other common aggregates
  PennDOT 2A: “cleaner”, minimal fines designed for drainage
  PennDOT 2RC: very wide spec that can contain dirt and organics
DGLVR
DSA Specification Changes
2A

## Slide 3
DGLVR
DSA Specification Changes
DSA
2A
 | 2” | 1.5” | ¾” | ¼” | 1/16” | “fines”
DSA |  | 100 | 65-97 | 30-65 | 15-30 | 10-15*
2A | 100 |  | 52-100 | 24-50 | 10-30 | 0-10

## Slide 4
DSA developed in 2000, modified over the years
Recent History
20015-18: implemented Plasticity index to limit clay content
2019: Increased max fine content for non-plastic aggregate
2022: reduced paver requirement to jobs over 500 tons
DGLVR
DSA Specification Changes

## Slide 5
Current Driving Surface Aggregate Specification
DGLVR
DSA Specification Changes
Passing Sieve | Lower % | Higher %
1½ inch | 100 | -
3/4 inch | 65 | 97
#4 (1/4 ") | 30 | 65
#16 (1/16 ") | 15 | 30
#200(1/200 ") | 10 | 15*
% passing by weight
* Up to 17 % fines if PI <2

## Slide 6
2020 Driving Surface Aggregate Specification
DGLVR
DSA Specification Changes
Passing Sieve | Lower % | Higher %
1½ inch | 100 | -
3/4 inch | 65 | 97
#4 (1/4 ") | 30 | 65
#16 (1/16 ") | 15 | 30
#200(1/200 ") | 10 | 15*
% passing by weight
* Up to 17 % fines if PI <2

## Slide 7
DGLVR
DSA Specification Changes
Passing Sieve | Lower % | Higher %
1½ inch | 100 | -
3/4 inch | 65 | 97
#4 (1/4 ") | 30 | 65
#16 (1/16 ") | 15 | 30
#200(1/200 ") | 10 11 | 15*
% passing by weight
* Up to 17 % fines if PI <2
Proposed Driving Surface Aggregate Change
  Proposing to increase #200 sieve to 11%

## Slide 8
  Question:
  Why are we proposing the change to 11%?
    Answer:
  In 2020 we tested 52 DSA piles
    15 failed
  20% of samples had #200 sieves that were ≤11%
  17% of samples has #200 sieves that were <11%
  In 2021 we tested 60 DSA piles
    5 failed
  23% of samples had #200 sieves that were ≤11%
  19% of samples has #200 sieves that were <11%
DGLVR
DSA Specification Changes

## Slide 9
  Question:
  Why are we proposing the change to 11%?
    Answer:
  In 2022 we tested 47 DSA piles
    7 failed
  38% of samples had #200 sieves that were ≤11%
  33% of samples has #200 sieves that were <11%
  Number of samples with low #200 results
  almost doubled in 2022!
DGLVR
DSA Specification Changes

## Slide 10
DGLVR
DSA Specification Changes
Chart: DSA Results 2020-2022
| #200 ≤11%
2020 | 20
2021 | 23
2022 | 38
Samples <11% in fines
Percentage of passing DSA Samples with <11% fines
2020
20%
2021
23%
2022
38%

## Slide 11
  Why are projects with #200 sieves <11% an issue?
  Most DSA issues in 2022 that were material-related (not placement) were due to low fines (10-11%).
  Raveling during and immediately after placement
  Grading and re-compaction required soon after new placement
  Multiple projects required remediation immediately after placement
    Time & Money…
We can’t reject material that meets spec, even 10.0%.
DGLVR
DSA Specification Changes

## Slide 12
DGLVR
DSA Specification Changes
  Road #1:
  10.4% #200 Sieve
  Immediately after placement & compaction
Most DSA issues in 2022 that were material-related (not placement) were due to low fine content (10-11%).
We can’t reject material that meets spec, even 10.0%.

## Slide 13
DGLVR
DSA Specification Changes
  Road #1:
  10.4% #200 Sieve
  Immediately after placement & compaction

## Slide 14
DGLVR
DSA Specification Changes
Take a closer look…

## Slide 15
DGLVR
DSA Specification Changes
Lack of fines
Loose aggregate

## Slide 16
DGLVR
DSA Specification Changes
  Road #1:
  10.4% #200 Sieve
  Immediately after placement & compaction
Lack of fines
Loose aggregate

## Slide 17
DGLVR
DSA Specification Changes
  Road #2:
  Low Moisture & Fines
  Immediately after placement & compaction

## Slide 18
DGLVR
DSA Specification Changes
  Road #2:
  Low Moisture & Fines
  Immediately after placement & compaction

## Slide 19
DGLVR
DSA Specification Changes
  Road #2:
  Low Moisture & Fines
  Immediately after placement & compaction

## Slide 20
DGLVR
DSA Specification Changes
  Road #2:
  Low Moisture & Fines
  Immediately after placement & compaction

## Slide 21
DGLVR
DSA Specification Changes
  Road #2:
  Low Moisture & Fines
  3 months after placement

## Slide 22
DGLVR
DSA Specification Changes
  Road #2:
  11% #200 Sieve
  Low Moisture & Fines
  3 months after placement

## Slide 23
DGLVR
DSA Specification Changes
Proposed 2023 Driving Surface
Aggregate Specification
  Proposing to increase #200 sieve to 11%
Passing Sieve | Lower % | Higher %
1½ inch | 100 | -
3/4 inch | 65 | 97
#4 (1/4 ") | 30 | 65
#16 (1/16 ") | 15 | 30
#200(1/200 ") | 11 | 15*
% passing by weight
* Up to 17 % fines if PI <2

## Slide 24
  Other DSA Specifications
  DCNR Currently has their own DSA specification
  PennDOT currently has their own DSA specification
  The three specs do not all match!
  Why? Changes were made to the SCC spec that were never reflected in other specs.
DGLVR
DSA Specification Changes

## Slide 25
  DCNR Bureau of Forestry
  Match SCC specification
    Increase #200 sieve to 11%
    Change LA Abrasion to 40%
    Minus #200 composition word change - “Lime kiln dust and cement kiln dust may be added to DSA to account for up to 50% of the fines passing the #200 sieve”.
  PennDOT
  Meeting with PennDOT to update spec to match SCC specification.
  Goal is to have the DSA specification be the same for all 3 entities!
DGLVR
DSA Specification Changes

## Slide 26
  Next Steps?
  Thoughts / Questions from CDs?
  Talking with PA Aggregate & Concrete Association in February for supplier input.
  Take proposed change to SCC for approval
  If approved, determine acceptable date for implementation.
DGLVR
DSA Specification Changes

## Slide 27
  DSA Notification Form
  Make sure you are using the most recent form!
    Dated 7/2022
  Please fill in the cost of the DSA
    Used to track $/ton
DGLVR
DSA Specification Changes